A study of the effects of surface roughness on amount of heat transferred

A Major Qualifying Project Report:

Submitted to the faculty of

Worcester Polytechnic Institute

In partial fulfillment of the requirements for the

Degree of Bachelor of Science

In Mechanical Engineering

Submitted by:

Michael R. Ayer

Approved by:

Professor Christopher A. Brown, Advisor

Surface Metrology Laboratory

Mechanical Engineering Department

Worcester Polytechnic Institute

Worcester, MA 01609

April 2010

Keywords: Surface Metrology, Heat Transfer

Table of Contents

Abstract	3

Introduction	4

Objective	4

Rationale	4

Solar hot water heaters	4

State-of-the-art	4

Approach	5

Methods	6

Test Box	6

Test Apparatus	7

Surface Texture Preparations	7

Surface Roughness Measurements and Area-scale Analysis	8

Testing using Apparatus	8

Measure Temperature using LabView	8

Results	10

Surface Processing	10

Surface Measurements	10

Temperature Test Results	10

Discussion	12

Surface Processing	12

Surface Measurements	12

Temperature Tests	12

Conclusion	13

Acknowledgements	13

References	13

# Abstract

Heat transfer is composed of convective, conductive and radiant heat transfer.   There are many variables that can affect heat transfer: size, type of material, etc.  Aluminum is a readily available test material that has very well documented properties and is easy to change the surface texture.  I will use a silicon based sand paper to polish the test materials.  The surface textures of the aluminum samples were measured using an Olympus LEXT 3100 scanning laser microscope.  Area-scale analysis was also used to determine at which scale the most heat transfer was observed.

# Introduction

## Objective

In heat transfer, whether it be conductive, convective, or radiant, area affects the amount of heat transferred.  As the area of the material changes the amount of heat transferred will change as well.  In the case of radiant heat transfer, the term emissivity is also affected by surface texture.  This is research will analyze the hyposthesis that modifying the surface texture will result in an increase in the amount of heat transferred.

By analyzing the final temperature of the test material with a varied surface texture after being exposed to a work lamp for thirty minutes we hope to be able to determine the scale at which the most heat was transferred.

## Rationale

## Solar hot water heaters

Aluminum is used in many applications that involve solar power.  One specific example is solar hot water heating, in some Solar hot water heaters an aluminum plate is used to absorb heat from the sun and transfer it to water that is being stored in a reservoir.  If one could increase the amount of heat being transferred to the water in the reservoir the system will then become more efficient.  The more efficient the system is the more money the person or business is saving.

## State-of-the-art

Not much research has been done on the affects of differences of surface roughness and how that correlates to amount of heat transferred.  To conduct my literary search for previously conducted research I used many different scholarly search engines such as: Lexis Nexis, Engineering Village, Science Direct, and Jstore.  The search terms included: Surface texture, surface texture and heat transfer, surface texture and absorptivity, surface texture and radiant heat transfer, and texture gradient and heat transfer.

## Approach

Since there has not been much research in the area I will have to devise my own test procedures.  This test procedure will be based on similar test procedures that are documented is ASTM E-744.  Changes to E-744 were made due to the scale of the test being performed and the costs of acquiring the test lamp. ASTM standard E-744 requires the use of a Xenon Arc lamp, which is expensive and hard to obtain.  The use of a Halogen work lamp was suggested to me by George Kelly of BP solar and was used in this research.  The test material used is T6061 aluminum, and will have its surface texture changed using silicon based sand paper.  Measurements of the surface will be taken using an Olympus LEXT 3100 scanning laser confocal microscope.  The lamp will be used to heat up the test material and LabView will be used to record temperature in respects to time.  This study will use area-scale analysis to compare relative area with respects to scale.

# Methods

## Test Box

The test box is an aluminum box that holds the test specimen.  The box is covered with a layer of Lexan, this is to allow the box the box temperature to be mostly affected by the light.  The box is also painted black to help absorb as much heat from the light.  In Figure 1 below is an illustration of the box suggested by ASTM E-744. Some modifications to the box where made to fit my research.  Test specimens were elevated off the bottom of the test box using microscope slides.  This would cut down on the amount of convective heat being transferred.  I also used two thermocouples instead of one.  One thermocouple was used to obtain the temperature of the test specimen but the second thermocouple was used to record the temperature of inside the box.  Again the thermocouple was elevated off the bottom of the box to cut down on convective heat being transferred from the box.  I also used a piece of aluminum foil to shield the thermocouple from the light.  This was to eliminate the light shining on the thermocouple itself, this could have increased the recorded temperature due to heat being transferred from the light to the thermocouple through radiation.

Figure 1: Test Box ASTM E-744

## Test Apparatus

An adapted test method was designed based off ASTM standard E-744. In standard E-744 a test box was prepared with a cover to house the test materials. Then one could choose to do an outdoor test or an indoor test.  I based my test apparatus off the indoor test suggested by E-744.  The Xenon arc lamp was used in E-744 as the heating source, after contacting ASTM and then being forwarded to George Kelly at BP Solar, I was informed that a cheaper and easier to obtain heat lamp would suffice for the test.  A Halogen Work lamp was used as a heat source in my experiments, with a 300 watt bulb.  The light was hung 6 inches from the test box and was angled to face down directly on the test box.  To take temperature data I needed to use a DAQ.  This DAQ converted the analog data being obtained by the thermocouples to digital data that could be read by my computer.  The DAQ was set up to measure the temperature of the test specimen while at the same time measuring the temperature of the box itself.  The test apparatus was then constructed in a dark room where no outside light would be able to affect the test specimen.

## Surface Texture Preparations

The test specimens are to have the dimensions width 2in. length 2in. and a thickness of .5in.  The surface of the test specimens were prepared using Silicon based sand paper, the sand paper was used to polish the aluminum. The normal specimen had no surface texture modification made.  The grit of the sand paper used was: 120, 240, 400 and 600. Picture of the test specimens are presented in the appendix.  Preparations to the surface were conducted by hand, this was to attempt to make the surface the same and help with repeatability.  First I would start using the roughest grit, 120, to polish the aluminum past the extrusion lines.  The extrusion lines for the normal were left intact, refer to the appendix.  Once past the extrusion lines I would change the sand paper to a finer grit periodically until reaching the final stage.  I then cleaned all specimens using isopropyl alcohol to clean the surface of dirt and particles that could have been left behind by the sandpaper.  After cleaning the specimen the weight was measured and recorded

## Surface Roughness Measurements and Area-scale Analysis

All surface roughness measurements were conducted using an Olympus LEXT 4000 laser scanning confocal microscope.  I used the fine acquisition setting to obtain all surface roughness data. All surface roughness measurements were obtained using 50X-magnification.  After obtaining topographical images of the surface I then converted them to a file that could be analyzed by the software SFRX.  I used SFRX to complete the area-scale analysis. The area-scale analysis used was bottom-left which was suggested to me by my advisor.

## Testing using Apparatus

Before testing the test specimen and the cover plate need to be cleaned, the cover plate also needed to be cleaned carefully as to not scratch it.  After connecting the thermocouples to the test specimen and the test box, turn off all lights and connect the DAQ to the computer that will be recording the data.  After sealing of the room with the test apparatus the test can begin.  All tests are to begin at room temperature and be exposed to the heat source for only 30 minutes.  I attached a thermocouple to the bottom of the test specimen using a hot glue gun.  I then placed the specimen on the test stand.  The thermocouple that measures the box temperature is fixed to the bottom of the box but the junction is raised off the bottom and is shielded by aluminum foil.

## Measure Temperature using LabView

To measure the temperature data of the test, a SCXI-1100 module from National Instruments was used.  This multi channel DAQ was perfect for taking two temperature measurements at the same time while also providing a time stamp for when the data was measured.  This is where I had a great deal of trouble, programming LabView to take multiple samples from multiple channels took longer than expected.  The figure below illustrates the block diagram of the VI I used to take my temperature measurements.  I then had LabView write all data points to Excel where I did my analysis.

Figure 2: LabView Block Diagram

# Results

## Surface Processing

The surfaces of the test specimens were prepared using different grit sand papers and manually polishing the specimen to the desired state.  To obtain the desired surface texture I first needed to polish the specimen past the extrusion lines left behind from forming of the aluminum bar stock.  Once this was achieved the grit of the sand paper was changed and the process repeats.  Once the desired surface texture is achieved the sample was cleaned and weighed.

## Surface Measurements

Using the Olympus LEXT 4000 to measure the surface I recorded data for all test specimens.  This was done using the 50X objective lens.  I determined which objective lens to use by measuring the roughness using 5X, 10X, 20X, and 50X.  After comparing the data from the measurements I decided that the 50X provided the most accurate readings.  A graph of the combined area-scale analysis is provided in the Appendix.  I then measured all test specimens with the 50X objective lens and compared the measured roughness.  In the Figure below is the area-scale graph of all test specimens at 50X.

## Temperature Test Results

Prior to testing, all test specimens were cleaned and at around room temperature.  The Figure below displays temperature-time plots for all test specimens.

Figure 3: Temp-Time

Each test did not start at the same temperature, the Figure below display change in Temperature-time plots for all test specimens

Figure 4: dTemperature-Time

# Discussion

## Surface Processing

Since the test specimens were prepared by hand there were some variances in the surface texture, most notable the corners.  In future tests I would suggest chamfering the edges, this will help make an even surface for the test specimen.  This experiment did not consider test specimens that were prepared with CnC machines.  In future tests I would suggest machining the surface of the test specimen with different end mills, noting the feet rates and step-overs for repeatability.  It is important to have an even surface texture.

## Surface Measurements

After compiling surface measurements from SP120 using the 5X, 10X, 20X, and 50X objective lens, it was decided that the 50X objective lens was best suited to take measurements.

## Temperature Tests

A difference in final temperature was observed between the test specimens.  Of the test specimens SP600 had the largest difference in temperature; this is most likely due to darkening of the test specimen during surface polishing.  The specimen with the second highest temperature difference was test specimen Normal.  There is a noticeable difference in how fast and the final temperature of the specimen after 30 minutes.  In future studies analysis could be performed to calculate the total amount of heat transferred, this can then be used to obtain the amount of radiant heat transferred.  After obtaining the amount of radiant heat transferred one could then study how surface texture affects emissivity. “Properties of emissivity strongly depend on surface conditions… This uncertainty is largely due to the difficulty in characterizing and describing the surface conditions precisely”. (P.889 TFS)  Also further analysis could be done pertaining surface texture and its effects on total amount of heat transferred.  In the Appendix are figures that display obtained temperature-time data and potential analysis of heat transferred.

# Conclusion

- Using silicon based sand paper can be used to change the surface texture of aluminum to test.  Pre-surface-processing techniques, such as chamfering of edges, can be implemented to promote an even surface texture for more accurate results.

- The higher the magnification of the objective lens the more accurate the area-scale analysis is.

- Changing the surface texture of aluminum causes a change in the amount of heat transferred.  The more rough the surface is the more heat that is transferred.

# Acknowledgements

The author acknowledges his advisor Professor C. A. Brown for his knowledge, support and guidance.  Olympus for the access to LEXT4000.  Brendan Powers for help with the lab and SFRX.  Finally Worcester Polytechnic Institute for providing me with a world class education.

# References