- Methods

  - Test Box

    - ASTM standard E-781 was used as a guide for the assembly of the test box.  The test box is an aluminum pan that was painted black on the interior as specified by the standard.  A cover for the box was constructed from a sheet of Lexan and used to prevent the interior temperature from being affected by outside sources other than the test lamp.  To minimize the effects of convective heat transfer on the test material glass spacers were used to raise the test material off the test box.  Glass spacers were used for their low surface area and low heat transfer coefficient.  A piece of aluminum foil was used to shield the thermocouple and prevent potential false readings from direct exposure to the test lamp.

  - Test Apparatus

    - The test apparatus encompasses the test box, the test lamp, and the data acquisition device.  The test lamp used is a 300-600 watt halogen lamp.  The ASTM standard calls for a Xenon Arc lamp.  Unfortunately a Xenon arc lamp is expensive and difficult to obtain.  George Kelly from BP solar suggested a Halogen work lamp, stating that the light produced is similar to that of natural light and is considerably less expensive than a Xenon Arc lamp.  Also Halogen work lamps are easily obtained at local hardware stores.

    - A data acquisition device (DAQ) was used to take temperature readings over time.  The unit was developed by National Instruments and uses the program, LabView, also developed by National Instruments. A  LabView VI was programmed to take temperature measurements of the box and the material simultaneously with respect to time.  I went through many iterations of the program and performed many tests to insure that the VI would collect data consistently and accurately.  After the programming the VI, I connected the DAQ to my computer and the test box.

  - Surface Texture Preparations

    - Four out of five aluminum test samples were prepared using Professor Li’s suggestion of silicon based sand paper as suitable for the polishing process.  One test sample was not polished to serve as a control.  Sand paper with grits ranging from 240 (coarse), 120, 400 and  600 (fine) were used.  The unfinished test materials hard large extrusion lines, created during manufacturing, that had to be polished down to provide a more uniform base.  To remove the extrusion lines, the 240 grit (coarse) sand paper was used.  After the extrusion lines were removed I moved to a finer grit sand paper until the scratches produced by the previous polish were replaced with finer ones.  This was repeated until reaching the desired texture.  It was also necessary to wash the test material with alcohol to remove dust and dirt from the surface prior to polishing

    - Surface roughness measurements were obtained using an Olympus LEXT OLS4000 Measuring Laser Confocal Microscope.  The LEXT OLS4000 was an ideal machine to use for this experiment because of the use of lasers as well as user friendly software.  The OLS4000 uses a 405nm laser to obtain high resolution measurements.  Lasers are used in microscopy to decrease the wave length of a light source, this allows for higher resolutions.  Each test material was cleaned before scanning with the microscope, to avoid false measurements.

    - After the measurements were made using the OLS4000 Area-scale analysis was used to display at what scale were the test materials affected the most by the roughened surface.  The software SFRAX was used to perform area-scale analysis on the test samples.

  - Testing using Apparatus

    - The test apparatus was assembled in a dark room to mitigate the effects of foreign light sources.  The test apparatus used thermocouples, wired into the box itself, for the temperature measurements, using my computer to store the collected data.  A long cable allowed me to keep my computer outside the test room and avoid interference with the test.  Each test ran for approximately 30 minutes, taking temperature readings about every 5 seconds.  The test began as soon as the lamp was turned on.  The box was allowed to cool for 30 minutes prior to testing each sample.  Since the temperature of the room would fluctuate it was important to have a temperature reading at the start of each test to compare the differences in temperature.

  - Measuring Temperature using LabView

    - I programmed my VI to take 2 samples every 5 seconds: test material and box temperature.  The test would run for 30 minutes, the VI would record the test materials initial temperature and final temperature as well as the test materials temperature every 5 seconds.  The data was then sent to my computer where I then converted to Excel format.  I chose to have readings every 5 seconds because the temperature increase in the test material was not rapid.

# Results

## Surface Processing

The surfaces of the test specimens were prepared using different grit sand papers and manually polishing the specimen to the desired state.  Using the sand paper proved to be effective but time consuming.  The process was also not uniform; it was difficult to produce the same texture throughout the test material.  The inconsistent texture of the test materials affected the results of the experiment.  Also while polishing a test sample using grit of 600, I noticed a discoloration in the material.  During polishing the test material became darker.  This also affected my results due to more energy being absorbed by the darker material.  The test material polished with 600 grit, SP600, was considered an outlier.  All test materials were weighed after polishing.

Figure 1

## Surface Measurements

Using the Olympus LEXT 4000 with the 50X objective lens to measure the surface roughness, data was recorded for all test specimens.  The objective lens used was determined by measuring the roughness using 5X, 10X, 20X, and 50X lenses.  After comparing the data from the measurements I decided that the 50X lens provided the most precise and accurate readings.  (A graph of the combined area-scale analysis is provided in the Appendix.)  I then measured all test specimens with the 50X objective lens and compared the measured roughness.  Figure (figure number) below shows the area-scale graph of all test specimens at 50X.

## Temperature Test Results

Prior to testing, each test specimen was cleaned and its initial temperature was recorded. Figure (figure number)  below displays temperature-time plots for all test specimens. Tables 1 and 2 display the final temperature ( Degrees Celsius) and the difference from initial and final temperatures respectively.

| Test Sample | Final Temp. ◦C |
| --- | --- |
| Normal | 45.104 |
| SP120 | 43.272 |
| SP240 | 41.158 |
| SP400 | 43.037 |
| SP600 | 51.009 |

| Test Sample | Difference in Temp ◦C |
| --- | --- |
| Normal | 18.997 |
| SP120 | 15.76 |
| SP240 | 14.158 |
| SP400 | 16.433 |
| SP600 | 24.988 |

Figure 2: Temp-Time

Each test did not start at the same temperature. Figure (figure number) below displays the change in Temperature-time plots for all test specimens

Figure 3: dTemperature-Time

# Discussion

## Surface Processing

Since the test specimens were prepared by hand there were some variances in the surface texture, most notably the corners.  In future tests, chamfering the edges will help make an even surface for each test specimen.  This experiment did not consider test specimens that were prepared with CnC machines.  In future tests I would suggest machining the surface of each test specimen with different end mills, noting the feed rates and step-overs for repeatability.  It is important to have an even surface texture.  Also it is important to have many test samples that were prepared under the same conditions, this should increase repeatability and accuracy.

## Surface Measurements

After compiling surface measurements from SP120 using the 5X, 10X, 20X, and 50X objective lenses, I decided that the 50X objective lens was best suited to take measurements.  The use of the 50x lenses was suggested to me by my advisor. Why?  What did you observe to lead you to this conclusion?

## Temperature Tests

A difference in final temperature was observed between the test specimens.  Of the test specimens, SP600 had the largest difference in temperature. This is most likely due to the darkening of the specimen during surface polishing.  The specimen with the second highest temperature difference was test specimen Normal, this is due to the surface not being polished using silicon based polishers  There is a noticeable difference in how fast the temperature rose and the final temperature of each specimen after 30 minutes.  In future studies, analysis could be performed to calculate the total amount of heat transferred.  This can then be used to obtain the amount of radiant heat transferred.  One should also consider not painting the test box black.  I observed in my experiments that the temperature of the box would exceed the temperature of the test material.  This caused heat to be transferred from the box to the test material convectively, which could have affected the test.  After obtaining the amount of radiant heat transferred, one could then study how surface texture affects emissivity. “Properties of emissivity strongly depend on surface conditions… This uncertainty is largely due to the difficulty in characterizing and describing the surface conditions precisely”. (P.889 TFS)  Also further analysis could be done pertaining surface texture and its effects on total amount of heat transferred.  In the Appendix there are figures that display obtained temperature-time data and potential analysis of heat transferred.

# Conclusions

- Silicon based sand paper can be used to change the surface texture of aluminum to test.  Pre-surface-processing techniques, such as chamfering of edges, can be implemented to promote an even surface texture for more accurate results.

- The higher the magnification of the objective lens the more accurate the area-scale analysis.

- Changing the surface texture of aluminum causes a change in the amount of heat transferred.  The more rough the surface is the more heat that is transferred

# Appendices

## Issues and Solutions

During this experiment may obstacles had to be overcome, in this section I will review trouble areas and ways in which I overcame them.  The first issue I faced was finding a previous ASTM standard that would fulfill the needs for my experiment.  One way to make this task easier would be to find a similar standard and contact the head of that committee.  They are very knowledgeable about that standard as well as connecting you with people that who developed the standard or people who are currently using the standard.  Another problem area was programming the VI used by labView which controlled the data collection for the experiment.  I went through many iterations before I reached the final product.  I would suggest manipulating an existing VI to conform to the needs of the experiment before programming one from scratch.