- Methods

  - Test Box

    - ASTM standard E-781 was used as a guide for the assembly of the test box.  The test box is an aluminum pan that was painted black on the interior as specified by the standard.  A cover for the box was constructed from a sheet of Lexan and used to prevent the interior temperature from being affected by outside sources other than the test lamp.  To minimize the effects of convective heat transfer on the test material glass spacers were used to raise the test material off the test box.  Glass spacers were used for their low surface area and low heat transfer coefficient.  A piece of aluminum foil was used to shield the thermocouple and prevent potential false readings from direct exposure to the test lamp.

  - Test Apparatus

    - The test apparatus encompasses the test box, the test lamp, and the data acquisition device.  The test lamp used is a 300-600 watt halogen lamp.  The ASTM standard calls for a Xenon Arc lamp.  Unfortunately a Xenon arc lamp is expensive and difficult to obtain.  George Kelly from BP solar suggested a Halogen work lamp, stating that the light produced is similar to that of natural light and is considerably less expensive than a Xenon Arc lamp.  Also Halogen work lamps are easily obtained at local hardware stores.

    - A data acquisition device (DAQ) was used to take temperature readings over time.  The unit was developed by National Instruments and uses the program, LabView, also developed by National Instruments.   LabView VI was programmed to take temperature measurements of the box and the material simultaneously with respect to time.  I went through many iterations of the program and performed many tests to insure that the VI would collect data consistently and accurately.  After the programming the VI, I connected the DAQ to my computer and the test box.

  - Surface Texture Preparations

    - Originally, the plan was to machine the test materials using CNC machines with predetermined feed rates and steps.  This process was later replaced with hand polishing of the test materials.   Professor Li  suggested a silicon based sand paper as suitable for the polishing process.    Sand paper with grits ranging from 240 (coarse) to 600 (fine) was used.  The unfinished test materials hard large extrusion lines, created during manufacturing, that had to be polished down to provide a more uniform base.  To remove the extrusion lines, the 240 grit (coarse) sand paper was used.  After the extrusion lines were removed I moved to a finer grit sand paper until the scratches produced by the previous polish were replaced with finer ones.  This was repeated until reaching the desired texture.  It was also necessary to wash the test material with alcohol to remove dust and dirt from the surface prior to polishing

  - Surface Roughness Measurements and Area-scale Analysis- where can I get information that I can site? ???  see below

  - Testing using Apparatus

    - The test apparatus was assembled in a dark room to mitigate the effects of foreign light sources.  The test apparatus used thermocouples,  wired into the box itself, for the temperature measurents. . I then connected my computer to the DAQ.  A long cable allowed me to keep my computer outside the test room and avoid interference with the test.  Each test ran for approximately 30 minutes, taking temperature readings about every 5 seconds.  The test began as soon as the lamp was turned on.  The box was  allowed to cool for 30 minutes prior to testing each sample.  Since the temperature of the room would fluctuate it was important to have a temperature reading at the start of each test to compare the differences in temperature.

  - Measuring Temperature using LabView

    - I programmed my VI to take 2 samples every 5 seconds: test material and box temperature.  The test would run for 30 minutes, the VI would record the test materials initial temperature and final temperature as well as the test materials temperature every 5 seconds.  The data was then sent to my computer where I then converted to Excel format

    - I chose to have readings every 5 seconds because the temperature increase in the test material was not rapid.

    - http://www.zemetrics.com/surface-roughness-measurement.shtml

    - http://www.optics.arizona.edu/jcwyant/pdf/Published_Papers/Optical_Testing/AbsoluteMeasurementOfSurfaceRoughness.pdf

    - http://ts.nist.gov/MeasurementServices/Calibrations/upload/89-4088.pdf

    - http://www.4m-net.org/KnowledgeBase/papers/2008/04-02

    - http://www.springerlink.com/content/67l57x088438q518/

    - http://www.wpi.edu/Pubs/E-project/Available/E-project-043007-085454/unrestricted/GrindingWheelSurfaceTextureCharacterizationUsingScaleSensitiveFractalAnalysis.pdf                           This is a paper submitted in pursuit of an undergraduate Mechanical Engineering Degree from WPI in 2007.  You might get ideas from it – just don’t copy from it without proper citation.