# Results

## Surface Processing

The surfaces of the test specimens were prepared using different grit sand papers and manually polishing the specimen to the desired state.  Using the sand paper proved to be effective but time consuming.  The process was also not uniform; it was difficult to produce the same texture throughout the test material.  The inconsistent texture of the test materials had an effect on the results of the experiment.  Also while polishing a test sample using SP600, I noticed a discoloration in the material.  During polishing the test material became darker.  This also affected my results due to more energy being abosrobed by the darker material.  The test material SP600 was considered an outlier.  All test materials were weighed after polishing.

## Surface Measurements

Using the Olympus LEXT 4000 to measure the surface, data was recorded for all test specimens.  This was done using the 50X objective lens. The objective lens used was determined by measuring the roughness using 5X, 10X, 20X, and 50X.  After comparing the data from the measurements it was decided that the 50X provided the most accurate readings.  A graph of the combined area-scale analysis is provided in the Appendix.  I then measured all test specimens with the 50X objective lens and compared the measured roughness.  In the Figure below is the area-scale graph of all test specimens at 50X.

## Temperature Test Results

Prior to testing, all test specimens were cleaned and initial temperatures were recorded.  The Figure below displays temperature-time plots for all test specimens.

Figure 3: Temp-Time

Each test did not start at the same temperature. The Figure below displays the change in Temperature-time plots for all test specimens

Figure 4: dTemperature-Time

# Discussion

## Surface Processing

Since the test specimens were prepared by hand there were some variances in the surface texture, most notably the corners.  In future tests  chamfering the edges will help make an even surface for each test specimen.  This experiment did not consider test specimens that were prepared with CnC machines.  In future tests I would suggest machining the surface of each test specimen with different end mills, noting the feet rates and step-overs for repeatability.  It is important to have an even surface texture.

## Surface Measurements

After compiling surface measurements from SP120 using the 5X, 10X, 20X, and 50X objective lens, i decided that the 50X objective lens was best suited to take measurements.

## Temperature Tests

A difference in final temperature was observed between the test specimens.  Of the test specimens, SP600 had the largest difference in temperature. This is most likely due to darkening of the test specimen during surface polishing.  The specimen with the second highest temperature difference was test specimen Normal.  There is a noticeable difference in how fast the temperature rose and the final temperature of the specimen after 30 minutes.  In future studies, analysis could be performed to calculate the total amount of heat transferred.  This can then be used to obtain the amount of radiant heat transferred.  After obtaining the amount of radiant heat transferred, one could then study how surface texture affects emissivity. “Properties of emissivity strongly depend on surface conditions… This uncertainty is largely due to the difficulty in characterizing and describing the surface conditions precisely”. (P.889 TFS)  Also further analysis could be done pertaining surface texture and its effects on total amount of heat transferred.  In the Appendix are figures that display obtained temperature-time data and potential analysis of heat transferred.

# Conclusion

- Silicon based sand paper can be used to change the surface texture of aluminum to test.  Pre-surface-processing techniques, such as chamfering of edges, can be implemented to promote an even surface texture for more accurate results.

- The higher the magnification of the objective lens the more accurate the area-scale analysis.

- Changing the surface texture of aluminum causes a change in the amount of heat transferred.  The more rough the surface is the more heat that is transferred.