# Results

## Surface Processing

The surfaces of the test specimens were prepared using different grit sand papers and manually polishing the specimen to the desired state.  Using the sand paper proved to be effective but time consuming.  The process was also not uniform; it was difficult to produce the same texture throughout the test material.  The inconsistent texture of the test materials affected the results of the experiment.  Also while polishing a test sample using grit of 600, I noticed a discoloration in the material.  During polishing the test material became darker.  This also affected my results due to more energy being absorbed by the darker material.  The test material polished with 600 grit, SP600, was considered an outlier.  All test materials were weighed after polishing.

## Surface Measurements

Using the Olympus LEXT 4000 with the 50X objective lens to measure the surface roughness, data was recorded for all test specimens.  The objective lens used was determined by measuring the roughness using 5X, 10X, 20X, and 50X lenses.  After comparing the data from the measurements I decided that the 50X lens provided the most precise and accurate readings.  (A graph of the combined area-scale analysis is provided in the Appendix.)  I then measured all test specimens with the 50X objective lens and compared the measured roughness.  Figure (figure number) below shows the area-scale graph of all test specimens at 50X.

## Temperature Test Results

Prior to testing, each test specimen was cleaned and its initial temperature was recorded. Figure (figure number)  below displays temperature-time plots for all test specimens.

Figure 3: Temp-Time

Each test did not start at the same temperature. Figure (figure number) below displays the change in Temperature-time plots for all test specimens

Figure 4: dTemperature-Time

# Discussion

## Surface Processing

Since the test specimens were prepared by hand there were some variances in the surface texture, most notably the corners.  In future tests, chamfering the edges will help make an even surface for each test specimen.  This experiment did not consider test specimens that were prepared with CnC machines.  In future tests I would suggest machining the surface of each test specimen with different end mills, noting the feed rates and step-overs for repeatability.  It is important to have an even surface texture.  Also it is important to have many test samples that were prepared under the same conditions, this should increase repeatability and accuracy.

## Surface Measurements

After compiling surface measurements from SP120 using the 5X, 10X, 20X, and 50X objective lenses, I decided that the 50X objective lens was best suited to take measurements.  The use of the 50x lenses was suggested to me by my advisor. Why?  What did you observe to lead you to this conclusion?

## Temperature Tests

A difference in final temperature was observed between the test specimens.  Of the test specimens, SP600 had the largest difference in temperature. This is most likely due to the darkening of the specimen during surface polishing.  The specimen with the second highest temperature difference was test specimen Normal, this is due to the surface not being polished using silicon based polishers  There is a noticeable difference in how fast the temperature rose and the final temperature of each specimen after 30 minutes.  In future studies, analysis could be performed to calculate the total amount of heat transferred.  (Is there a formula that can be inserted here?) This can then be used to obtain the amount of radiant heat transferred.  (another formula here?) After obtaining the amount of radiant heat transferred, one could then study how surface texture affects emissivity. “Properties of emissivity strongly depend on surface conditions… This uncertainty is largely due to the difficulty in characterizing and describing the surface conditions precisely”. (P.889 TFS)  Also further analysis could be done pertaining surface texture and its effects on total amount of heat transferred.  In the Appendix there are figures that display obtained temperature-time data and potential analysis of heat transferred.

# Conclusions

- Silicon based sand paper can be used to change the surface texture of aluminum to test.  Pre-surface-processing techniques, such as chamfering of edges, can be implemented to promote an even surface texture for more accurate results.

- The higher the magnification of the objective lens the more accurate the area-scale analysis.

- Changing the surface texture of aluminum causes a change in the amount of heat transferred.  The more rough the surface is the more heat that is transferred.   Is there any formula that describes this heat transfer?   Since the samples didn’t start the heating process at the same temperature, do you have graphs that plot the actual start and end for each sample and the “normalized or adjusted” plots for comparison, or are those graphs figures 3 and 4?  Would doing multiple tests for each sample have aided in improving the consistency of the results?  How about having multiple samples of each roughness?  If you did multiple tests or had multiple samples, you might want to graph them to show how the data was “normalized.  Since the samples did not start at the same temperature, did the data or you studies provide any indication of whether or how the test results were affected?  I would expect that a sample that started at a higher temperature might take longer to reach its final temperature or might not have as great a difference between the start and end temperatures at the end of the test.  How would you compensate for this effect?