## Slide 1: Mean-Value Method of Lateral Force Calibration
A Major Qualifying Project
By
Derek Eggiman

## Slide 2: Introduction

## Slide 3: Acknowledgments
We would like to thank Sigma-Xi for generously funding this project.
We would also like to thank Professor Nancy Burnham and Dr. Deli Liu.

## Slide 4: Atomic Force Microscope
Focused laser is reflected off cantilever.
Changes in cantilever orientation result in a change of laser position
Laser position is detected by the photo diode.
Cantilever position is interpolated from photo diode signal.

## Slide 5: Current Problems in LFM Calibration
Many studies assume a functional form for friction, f=μ(N+A).
Other methods calibrate as a function of load.
  Repeated scans
  Excess tip wear.
Other methods require special equipment or are far to complicated and time consuming.
Want quick, in-situ method.

## Slide 6: MethoDology
Equilibrium equations depend on direction of motion (Vx) and angle (θ).
Taking the average value of scans in opposite directions over the same surface results in cancelations.
Flat-avg= Floadtan(θ) or
Vlat-avg= αFloadtan(θ)

## Slide 7: Results & Discussion

## Slide 8: Samples:Tested
Piano wire
Steel rod
Solder spheres
1.588 mm diameter Si3N4 ball bearings
http://www.satotekkou.co.jp/en/product/img/ceramic-p04.jpg

## Slide 9: Single ScaN: Topography & LFM

## Slide 10: Single Scan: Re-plot

## Slide 11: Experimental Difficulties
Finding a sufficiently smooth surface
Lack of lateral force sensitivity
Crosstalk of lateral and normal force signals

## Slide 12: Crosstalk

## Slide 13: Full scan Mean-value analysis
Obtained by taking a complete image of 256X256 data points in a 27 X 27 (μm) scan range.
Then taking the mean value along the y axis and using this data to perform our analysis.
Plotted the mean value of:
  Topography (μm)
  LFM Forward
  LFM Reverse

## Slide 14: Full Scan: Topography

## Slide 15: Full Scan: LFM

## Slide 16: Full Scan: Re-plot

## Slide 17: Conclusions
Mean value of 256 X 256 point scan shows high degree of linearity. R2=0.961.
Successfully derived proof of concept.
Work will be continued by Saonti Chakraborty and published in a peer reviewed journal.

## Slide 18: Questions?
http://www.phdcomics.com/comics/archive.php?comicid=771